## Slide 1
THE TEN COMMANDMENTS OF INJECTION MOLDING

## Slide 2
COMMANDMENT #1: UTILIZE CONSTANT WALL THICKNESS
  Constant wall facilitates material flow – no eddying…
  Facilitates cooling – thickest section dictates cooling time
    2x wall = 6x to 8x cool time
  Sink – materials shrink according to how thick they are
  AVOID – thin to thick to thin (thick to thin okay, to a point…)
sink

## Slide 3
  CYCLE TIME- BASELINE
    Depends on part / wall thickness – approx. 80% of the cycle time is cooling (pack/hold/cool/recover)
    Wall thickness is second order to cycle time, and first order to weight
      Cutting wall by 20% reduces weight by ~20%
      Current wall by 20% reduces cycle by ~40%
COMMANDMENT #1: UTILIZE CONSTANT WALL THICKNESS

## Slide 4
  Ribs add local structure
    Height gives 3rd order increase in strength
  Thickness at root should be 50% - 60% of nominal walls
  Look for thin steel conditions (gap <2t)
  Look for places where design is weak locally to reinforce with ribs
    don’t overdesign/overcompensate!!
COMMANDMENT #2: UTILIZE RIBS AND BOSSES FOR STRUCTURE

## Slide 5
  Bosses add local structure
  Great opportunity for sink if done poorly
COMMANDMENT #2: UTILIZE RIBS AND BOSSES FOR STRUCTURE

## Slide 6
  Outside radii should be no smaller than the smallest cutter from the machine shop (ask your moldbuilder)
  Allows easier flow of material through mold
  Radii reduce stress concentration in molded parts
COMMANDMENT #3: AVOID SHARP CORNERS
AND TRANSITIONS

## Slide 7
  What do sharp corners cause on molded parts?
    Flow anomalies (eddying) will certainly occur
    Stress concentrators
    CNC cutters can’t make them in steel – must be (longer / more $)
COMMANDMENT #3: AVOID SHARP CORNERS
AND TRANSITIONS

## Slide 8
THIN STEEL / SECTION CONDITIONS
  Forces of up to 18kpsi on a thin section – not good
  Thin plastic sections are weaker
  Thin steel sections / gaps are harder to machine
COMMANDMENT #4 – AVOID THIN SECTIONS / THIN STEEL

## Slide 9
BEWARE OF SIDE ACTION – BUT IF YOU MUST, MAKE THE PART MULTIFUNCTIONAL
  Slides / hydraulic cylinders / horn pins - must move steel out of the way to clear for ejection
  Adds cost / complexity / failure modes to the mold
  Will cause premature wear
  Adds cycle time – increased cost at part level!
COMMANDMENT #5: AVOID UNDERCUTS / MOLD SIDE ACTION

## Slide 10
BEWARE OF SIDE ACTION – BUT IF YOU MUST, MAKE THE PART MULTIFUNCTIONAL
  A lot of drawbacks here…
    Complicates mold
    Increases mold cost
    Decrease mold life
    Increases cycle time
    Increases press size, potentially
  BUT
    Might reduce number of parts, failure modes – DFMA!!
HORN PIN
HYDRAULIC / PNEUMATIC
COMMANDMENT #5: AVOID UNDERCUTS / MOLD SIDE ACTION

## Slide 11
COMMANDMENT #6: USE ADEQUATE DRAFT
USE ADEQUATE DRAFT
  Draft is taper that allows part to eject from mold
  Varies depending on
    Geometry
    Texture
    material

## Slide 12
TOLERANCE FOR PROCESS CAPABILITY
  Extremely tight tolerances add unnecessary cost, and in some cases preclude part from being manufactured
  SPI (Society of the Plastics Industry - plastics trade organization) publishes tolerance charts for various dim types, by material, with graphs corresponding to nominal dim
COMMANDMENT #7: TOLERANCE FOR PROCESS CAPABILITY

## Slide 13
UTILIZE FLOW RATIOS (FLOW PATH / THICKNESS)
  Simple calculation to help ensure parts fill properly – lower is better
  Do your best guess on path without MFA; ballpark is good enough
  Refer to table below; if your FL is too high, either
    thicken wall (bad)
    add/move gates (better)
COMMANDMENT #8: USE SIMPLE CALCULATIONS AND
MOLDFLOW ANALYSIS TO PREDICT BEHAVIOR

## Slide 14
USE MOLD FLOW ANALYSIS TO PREDICT FLOW PATTERNS
  Can show locations of knit lines, air traps, potential short shots – based on selected locations / quantity of gates
  Insight into molding pressure and cycle time – requiring design changes
COMMANDMENT #8: USE SIMPLE CALCULATIONS AND
MOLDFLOW ANALYSIS TO PREDICT BEHAVIOR

## Slide 15
KNIT LINES / SHORT SHOT
  Knit Lines - The location where melt fronts come together
    A function of gate location(s) and geometry
    Approx. 75%-80% of the strength of the section right next to it
    Cannot eliminate them!!!
    Particularly an issue with translucent / clear parts
  Short Shot – melt cools before full fill can be obtained
    MFA can predict this relatively well
    Weigh part and compare to 3D CAD weight
COMMANDMENT #9: BEWARE OF KNITS LINES
AND POTENTIAL SHORT SHOTS

## Slide 16
CONSIDER PEG – AND PROVIDE LOCATIONS IF NECESSARY (PADS)
  Gate locations / type
  Ejector Pin locations
  Parting Line
EJECTOR PINS (YELLOW)
COMMANDMENT #10: OPTIMIZE GATE LOCATION / TYPE
TO REDUCE MOLDED IN STRESSES AT GATE

## Slide 17
THE TEN COMMANDMENTS OF INJECTION MOLDING